ACETAL DELRIN

ACETAL DELRIN

We stock both the homopolymer, Acetal Delrin, and the copolymer, Acetal. Acetal Delrin and Acetal grades are dissimilar in that the former has improved mechanical properties whilst the Acetal grade has a superior resistance to alkalis. Both grades are not suited to components that need to be liquid and gas proof. For such components, it is recommended to opt for Pet-P material.

ACETAL DELRIN PROPERTIES

Excellent in:

Resilience

Machineability

Good in:

Fatigue strength

Dimensional stability

Mechanical strength

Hardness/stiffness

Rigidity

Impact strength (and at low temps.)

Wear resistance

Creep resistance

Electrical insulation

Chemical Resistance

Also suitable for:

Food contact

ACETAL DELRIN APPLICATIONS

• Gear wheels

• Bearings and heavy loaded bearings

• Valves and valve seats

• Electrical components

• Guide and wear strips

• Snapfit assemblies

• Pump Housings

• Impellers